**Iroko**

Family Name: Moraceae

Latin Name: Chlorophora Excelsa

Origin: Africa - Tropical

Strength Class: D40

Weight: Approx 660 kg/m³

Durability: Very Durable

Description: Golden Yellow in colour which darkens over time. Dense timber, with an interlocked grain. Has a medium to coarse texture with open pores.

Mechanical Dries well and fairly quickly, with only a slight tendency of

Properties: splitting. Moderate steam bending. Glues and finishes well.

Main Uses: Marine Work Cabinet Work

 Piling Cladding

 Boat Building Decking

 Furniture Flooring

 Joinery